# APOMUL STC

APOMUL STC is a polyvinyl acetate emulsion, stabilized with poly vinyl alcohol especially designed to be used as stiffening agent for textile finishing, and board laminations where good touch required.

TYPICAL PROPERTIES

Solid content %				43 (+) or (-) 1 %

Chemical basis			           Polyvinyl acetate

Protective colloid				Polyvinyl alcohol

Appearance 					Milky emulsion

pH						5  (+) or (-)  1

Viscosity at 30° C				30000 ±10000 cps

(Brookfield Viscometer, spindle # 7 @ 20 rpm)

Film clarity				           clear

Water resistance 				Good

Mechanical stability			Excellent

High temperature stability		Good

Resistance to air and humidity		Excellent

Resistance to wash                                   Excellent

HANDLING PRECAUTIONS

There is no health risk in handling APOMUL STC  The usual precautions in handling chemicals should be observed and it is recommended that operatives should wear goggles and gloves when handling the product. Any contact with the skin or eyes should be washed immediately with copious amount of cold water.

Please stir well before use.

Keep @ temperature max. 40°C.

Page 1 of 1